## Slide 1
2024 International Workshop on Magnetic Crystallography
Introduction to Magnetic Neutron Diffraction
A Tool for Magnetic Structure Determination
Outline
Magnetic Neutron Diffraction
Magnetic Lattice and Symmetry Element
Reflection Condition
Qingzhen HUANG
China Spallation Neutron Source
24-30 November 2024

## Slide 2
Magnetic Neutron Diffraction

## Slide 3
The neutron contains one “up” quark with +2/3 electron charge and two “down” quarks with -1/3 electron charge each, so neutron is a neutral particle.
有序磁结构的中子衍射
neutron
Neutron - a Subatomic Particle
Wave-particle Duality
M-diffraction
Because the neutron carries a magnetic moment of -1.913 mN (where mN is the nuclear magneton) and therefore it interacts with magnetic entities in materials. If the magnetic entities are disordered, then the magnetic diffuse scattering results. If they are in some way ordered then the magnetic structure can be studied via the magnetic Bragg reflections that arise. The magnetic reflections may or may not coincide with nuclear Bragg reflections.
There are three techniques are used to determine structure, X-ray, electron, and neutron diffraction. However, only neutron diffraction techniques can be used to determine magnetic structure. Although neutron is a neutral particle, it has a small magnetic moment. And it interacts with magnetic entities in material.

## Slide 4
1. Diffraction position: d =l/ 2sinq
2. Diffraction intensity: Ihkl = CFhkl
3. Structure factor: Fhkl
The expression of structure factors is basically the same, only different in electric scattering factor (f) for X-ray, neutron scattering length (b) for neutron, and ordered magnetic moment (m) and magnetic form factor (fM) for magnetic neutron diffraction.
Position, Intensity, and Structure Factor for
Nuclear & Magnetic Powder Diffraction
M-diffraction
Peaks Position: 2dhkl sinqhkl = nl
where l is the incident beam wavelength, d and q are the distance between successive hkl planes and Bragg angles of reflections, respectively.
Diffraction Intensity: Ihkl = CFhkl
where Fhkl is the hkl reflection amplitude of the diffracted X-ray, or neutron, or magnetic, and C is all others.
X-ray: Fhkl = |∑ fj exp(2p i (hx + ky + lz))|2 e-2W
where fj is the atomic scattering factor of atom j for X-ray.
Neutron: Fhkl = |∑ bj exp(2p i (hx + ky + lz))|2 e-2W
where bj is the neutron scattering length for atom j.
Magnetic: Fhkl = |∑ mj fMj exp(2p i (hx + ky + lz))|2 e-2W
where qj and fMj are the magnetic interaction vector and the
magnetic form factor for atom j, respectively.
2
2
2
2
2
This slice shows the comparing the powder diffraction of nuclear from magnetic. As you can see that they are highly similar, except the neutron scattering factor b and magnetic moment m. for neutron.

## Slide 5
Ihkl = C MT A(qB) [(g e2)/(2mc2)]2 <1-(e · K)2> Fhkl
C: Instrumental constant
MT : Multiplicity (for powder)
A(qB): angular factor, 1/(sinq sin2q)
[(g e2)/(2mc2)]=-0.27 : neutron-electron coupling
<1-(e · K)2>: orientation factor
Fhkl : Magnetic structure factor
Fhkl = | å m f exp[2p i (hx + ky + lz)]|2e-2W
m : magnetic moment
f : magnetic form factor
W:Debye Waller factor
Peaks Position: 2dhkl sinqhkl = nl
Diffraction Intensity:
h, k, l : reflection indexes
x, y, z : atomic coordinates
Magnetic sacttering
Magnetic moment, magnetisation vector, and scattering vector
<1-(e · K)2>: orientation factor
2
2
M-diffraction
q2=1-(e · K)2=1-cos2a=sin2a
q is magnetic interaction vector
Similar to diffraction from nuclear structure, the magnetic diffraction peak position represented by Bragg equation, here the hkl may/may not be the same as the nuclear structure due to the magnetic unit cell may/may not be the same dimension as nuclear one.
Because magnetic moment is a vector, an ordered moment contributes to each hkl is different. In equation of magnetic diffraction intensity Ihkl, the magnetic moment orientation factor defined q= e (e · K)-K is introduced, where e is scattering vector which is perpendicular to scattering plane hkl, and K is magnetization vector. q2=1-(e · K)2=1-cos2a=sin2a, if the moment parallel the scattering vector, i.e. a=0, then q=0 and Ihkl =0 .
hkl

## Slide 6
Magnetic intensities
Magnetic neutron diffraction and form factor for 3d and 4f elements
Magnetic intensities
有序磁结构的中子衍射
Magnetic form factor for Mn3+
Magnetic form factor for Er3+
Influence of magnetic form factor on diffraction peak strength
Figures a, d, and e are the magnetic form factor for d and f electrons and Mn3+ and Er3+ ions, respectively.
Plots b and c show the magnetic diffraction intensities for a Mn3+ contains and for a Er3+ contains compounds. The pattern fitted with nuclear structure model only (red line), and the differences shown at the lower part of figure are the magnetic diffraction intensities (blue line) .
Fitted by nuclear only
Fitted by nuclear only
Mn3+
Er3+
a
b
c
d
e
Magnetic: Fhkl = |∑ mj fMj exp(2p i (hx + ky + lz))| 2 e-2W
2

## Slide 7
m1≠m2, |m1|=|m2|
m1≠m3, |m1|≠|m3|
m2≠m3, |m2|≠|m3|
m1 & m2 anti-parallel
m1 & m3anti-parallel
m2 & m3 parallel
m1≠m2, |m1|≠|m2|
m1 & m2 anti-parallel
m1=m2
m1≠m2, |m1|=|m2|
m1x≠m2x, |m1x|=|m2x|
m1x & m2x anti-parallel
m1y=m2y
(a) Moment m is a vector
m
mx
my
m1≠m2, |m1|=|m2|
m1x≠m2x, |m1x|=|m2x|
m1 & m2 antiparallel
m1≠m2 ≠m3 ≠m4
|m1|=|m2|=|m3|=|m4|
m1x=m2x, m3x=m4x,
m1x & m2x; m3x & m4x ;
m1y,& m3y anti-parallel
m1y,& m2y ; m3y & m4y
parallel
m1
m2
m3
m1≠m2 ≠m3
|m1|=|m2|=|m3|
m1≠m2 ≠m3
|m1|=|m2|=|m3|
(c) Ferromagnetic
(d1) Ferrimagnetic
(d2) Ferrimagnetic
(e) Canted
ferromagnetic
(f) Antiferromagnetic
(g) Canted
antiferromagnetic
(h) Triangular
(i) Umbrella
mi≠mi+1≠mi+j
|mi|=|mi+1|=|mi+j|
(j) Incommensurate
(b) Paramagnetic
&diamagnetic
mi≠mi+1≠mi+j
|mi|≠|mi+1|≠|mi+j|
Schematic diagram
Schematic Diagram of Spin Disorder and Order
Schematic of the disorder and order magnetic structure in materials. The features of magnetic moment direction and magnitude for each diagram is shown.
MFM

## Slide 8
Spin disorder
Paramagnetic state
Diamagnetic state
No magnetic peaks
有序磁结构的中子衍射
Spin Disorder: Paramagnetic Neutron Diffraction
M-diffraction
LaMnO3
at 300 K
The disordered magnetic diffraction contribute on background.

## Slide 9
(1) Magnetic cell has the same as the cell dimension of the nuclear one;
(2) Magnetic peaks superpose on the nuclear peaks.
(100)
有序磁结构的中子衍射
Ferromagnetic order
M-diffraction
La0.7Ca0.3MnO3
At 50 K
Nuclear fit only

## Slide 10
(001)
有序磁结构的中子衍射
Antiferromagnetic order
M-diffraction
LaMnO3
at 50 K
Nuclear fit only
1. When the magnetic unit cell has the same dimension as the crystal unit cell with the space group contains primitive lattice (P), and do not have micro-symmetric element, such as P2/m, P222, P4/m, P622, Pm3m, etc., the magnetic reflection will appear at the Bragg position or overlap with nuclear peak.
2. For super magnetic cell, the magnetic diffraction peaks appear at the positions of the Bragg peak position of the magnetic supercell.

## Slide 11
The crystallographic primitive unit cell is indicated by solid lines and the dotted lines show the possible magnetic unit cell. aN = bN are the lattice parameters for the nuclear structure and aM and bM are those of the magnetic unit cell.
Ferromagnetic order;
Ferrimagnetic order;
Canted ferromagnetic order;
Collinear antiferromagnetic order;
Canted non-collinear antiferro-magnetic order where both the Mx and My directions have antiparallel components;
Example of a triangular antiferro-magnetic structure in hexagonal and trigonal crystals.
Example of super magnetic cell
M-dif.

## Slide 12
M-super-cell
1: (1/2,0,1/2)
2: (1/2,1,1/2)
3: (1/2,1,3/2)
4: (1/2,0,5/2)
(3/2,1,1/2)
5: (1/2,1,5/2)
(1/2,2,1/2)
6: (3/2,0,5/2)
(1/2,2,3/2)
7: (1/2,0,7/2)
(3/2,1,5/2)
(3/2,2,1/2)
Magnetic unit cell with propergation vector (1/2,0,1/2), i.e. aM=2aN, bM=bN, cM=2cN
Indexed by nuclear unit cell
i.e. aM=aN, bM=bN, cM=cN
1: (101)
2: (111)
3: (113)
4: (105)
(311)
5: (115)
(121)
6: (305)
(123)
7: (107)
(315)
(321)
有序磁结构的中子衍射
AFM: M-cell has an enlarged cell
N-cell
a
c
M-cell
10
20
30
40
50
60
0
2q(degree)
(a) At 25 K a broaden peak is observed at near at 2q=9° indicating a short-range magnetic order.
(b) A group long-range ordered magnetic diffractions appear at low-angle and they can be indexed by an enlarged nuclear unit cell.
Short-range order magnetic peak

## Slide 13
Differences show the magnetic diffraction pattern
Canted ferromagnetic structure
有序磁结构的中子衍射
Canted ferromagnetic order
For a canted ferromagnetic structure, the moment can be decomposed into two components: ferromagnetic and antiferromagnetic. Therefore, its diffraction peaks may appear at all Bragg positions.
M-dif.
AFM
FM
Nuclear
fit only
Two components
*
#
*
#

## Slide 14
*International tables for crystallography, Vol. D, 107 (2006).
Schematic diagram
(a) an antiferromagnetic helix
(b) a cone spiral
(AFM helix + FM)
(c) a cycloidal spiral
(d) a longitudinal spin-density wave
(e) a transverse spin-density wave
Helical and sinusoidal magnetic
Schematic Diagram of Incommensurate Spin Order
A specific feature for incommensurate is that the magnetic unit cell volume is not a rational number and that the period of the magnetic helix, spiral, and wave are not a multiple of the period of the lattice. A common characteristic of incommesurate magnetic structures is that the change of their magnetic moments has a Sine curve.
c
MFM

## Slide 15
NdMn2Ge2 at 240 K
Nuclear: I4/mmm
Magnetic: I4/mm’m’
FM with Nd moment in c-direction
(101)
(101)
Nuclear
fit only
(101) FM-Magnetic + Nuclear
240 K
140 K
400 K, Nuclear
有序磁结构的中子衍射
Incommensurate magnetic satellite peaks
(101)-
(101)+
Satellite
magnetic peaks
M-cell
NdMn2Ge2 at 240 K

## Slide 16
The magnetic scattering at low temperatures, indicating the development of two-dimensional long-range magnetic order. The solid curve is a fit assuming long-range order within the ab plane, and no correlations between planes.
Broad distribution of magnetic scattering at intermediate temperatures, indicating the development of short-range correlations in SrHo2O4. This scattering begins to develop below ,40K.
H. Karunadasa, Q. Huang, B. G. Ueland, J. W. Lynn, P. Schiffer, K. A. Regan, and R. J. Cava. PRB, 71, 144414 (2005)
The temperature dependence of the inverse magnetic susceptibility for SrHo2O4 between 320 K and 2 K. Data taken on cooling in an applied field of 50 Oe. Inset: detail of the inverse susceptibility in the low-temperature region.
在降温过程中，SrHo2O4经历短程磁有序(a)，继而在低于~3 K经历长程二维磁有序转变(b)。
， et al.
二维磁有序粉末衍射分析参考文献
有序磁结构的中子衍射
Short-range and Two-dimension Magnetic Order in SrHo2O4
M-diffraction

## Slide 17
Magnetic Lattice & Symmetry Element
Reflection Condition

## Slide 18
 | Crystal | Magnetic
Crystal system | 7 | 7
Bravais lattices | 14 | 36
Point groups | 32 | 122
Space groups | 230 | 1651
Since magnetic moment is a vector and antiferromagnetic is introduced,14 Bragg lattices, 32 point groups, and 230 space groups for crystal structure now become to 36, 122, and 1651 for magnetic structure, respectively.
Number of Nuclear & Magnetic Crystal system, Lattice,
and Symmetry Group
MLRC

## Slide 19
Pa nma
Pb nma
Pc nma
PA nma
PB nma
PC nma
PI nma
Magnetic space groups under #62: Pnma
* Paramagnetic
*Pnma1’
Pnma
Pn’m’a
Pnm’a’
Pn’ma’
Pn’m’a’
Pn’ma
Pnm’a
Pnma’
Magnetic space group
M-space group

## Slide 20
The W & B-lattice are expressed by two-letter symbols, a prime symbol (P, C, A, I, and F) of W-lattice followed by a subscript (A, a, C, c, I, and s) which indicates the location of the origin of the black lattice. The capital subscript letters A, C, and I indicate that the origins of the B-lattices are at the A-face center (0, b/2, c/2), C-face center (a/2, b/2, 0), and I-body center (a/2, b/2, c/2), respectively. The lower-case subscript letters a and c indicate the origin of the black lattice that are at the center of a-axis (a/2) and c-axis (c/2) of the white lattices, respectively. For example, the lattice PC is a combination of a P W-lattice with a P B-lattice with the origin at the C-center (½, ½, 0) of the W-lattice. The Pc indicates the origin of the P B-lattice at c/2. These types of magnetic lattices were applied to the seven crystal families giving a total of 36 magnetic lattices of which 14 are pure white and 22 are W & B lattices.
MSERC
Type of black & white magnetic lattice
There are five types of magnetic structure lattice (white-lattice) as well as that for crystal lattice. When the antiferromangnetic is introduced, 14 new types of magnetic lattice are generated, called White & Black lattice (W&B-lattice).

## Slide 21
W
W
W
W
W
W
W
W
W
W
W
W
W
W
13.
When introducing antiferromagnetic, the 14 nuclear Bravais lattices become 36 magnetic lattices in seven crystal systems, among which 14 ferromagnetic lattices (white) and 22 antiferromagnetic lattices (white & black).
MLRC
36 Magnetic Bravais Lattices
14 Trivial (white, FM) and 22 Nontrivial Magnetic Bravais Lattices (white & black, AFM)

## Slide 22
36 Magnetic Bravais Lattices, including 14 white (FM) and 22 white & black (AFM)
Triclinic
Monoclinic
磁结构点阵, 磁单胞
In the 36 W&B magnetic lattices in seven crystal systems, the relationship between the coordinate of magnetic lattice and that of the crystai system is indicated. The coordinate sytem for magnetic structure adopts the Cartesian coordinate system, here the b-axis of the triclinic and monoclinic crystal system is defined as the y-axis of the magnetic Cartesian coordinate system, while oblique coordinate system is used for the hexagonal and the rhombohedral systems.

## Slide 23
P114
The 36 Magnetic Bravais Lattices, 14 white (FM) and 22 white & black (AFM) continue
Orthorhombic
磁结构点阵, 磁单胞

## Slide 24
P115
The 36 Magnetic Bravais Lattices, 14 white (FM) and 22 white & black (AFM) continue
磁结构点阵, 磁单胞
Tetragonal

## Slide 25
The 36 Magnetic Bravais Lattices, 14 white (FM)and 22 white & black (AFM) continue
Rhombohedral
Hexagonal

## Slide 26
P116
The 36 Magnetic Bravais Lattices, 14 white (FM)and 22 white & black (AFM) continue
Cubic

## Slide 27
Crystal system | Symbols of families | Conventional coordinate system |  | Symbols of the 36 magnetic lattices | 
 |  | Restrictions on cell parameters | Parameters to be Determined | 14 (White) | 22 (White & Black)
Triclinic | a |  | a, b, c, a, b, g | aP | aPs
Monoclinic | m | a = g = 90°, | a, b, c, b, | mP, mC | mPb , mPa , mPC , mCc , mCa
Orthorhom-bic | o | a = b = g = 90° | a, b, c | oP, oI, oF (oC, oA) | oPI , oFs , oIc , (oPC , oPA), (oCA , oAC) (oPc , oPa), (oCc , oAa), (oCa , oAc)
Tetragonal | t | a = b, a = b = g = 90° | a = b ¹ c, | tP, tI | tPc , tPC , tPI , tIc
Hexagonal | h | a = b, a = b = 90°, g = 120° | a, c, | hP | hPc
Trigonal | h | a = b = c, a = b = g | a, a | hR | hRI
Cubic | c | a = b=c, a = b = g = 90° | a | cP, cF, cI | cPI , cFs
MSERC
Table of magnetic symmetry family, restriction on cell parameters, parameters to be determined, and symbols of the 14 white and 22 white and black magnetic lattices.

## Slide 28
(001)
(010)
(100)
(111)
(012)
(021)
(102)
(120)
(003)
(201)
(210)
(122)
(113)
(030)
(011)
(110)
(101)
(002)
(020)
(112)
(200)(121)
(022)
(103)
(211)
(202)
(031)
(hkl): h+k+l=2n
(0kl): k+l=2n
(h0l): h+l=2n
(hk0): h+k=2n
(00l): l=2n
(0k0): k=2n
(h00): h=2n
(hkl): h+k+l=2n+1
(0kl): k+l=2n+1
(h0l): h+l=2n+1
(hk0): h+k=2n+1
(00l): l=2n+1
(0k0): k=2n+1
(h00): h=2n+1
I
PI
(I’ )
Reflection Conditions for Magnetic lattices I and PI
MSERC
The body centred lattice I has ferromagnetics with the general reflection condition is h+k+l=2n, the same the nuclear one.
The primed body centred lattice I’ or PI has antifferromagnetics, i.e. the atom (ion) at (½, ½, ½) is antiparallel arrangement with the one at (0 0 0). The general reflection condition is h+k+l=2n+1.

## Slide 29
(001)
(110)
(002)
(111)
(112)
(021)
(020)
(003)
(200)
(022)
(201)
(113)
(202)
(220)
C
(hkl): h+k=2n
(hk0): h+k=2n
(0kl): k=2n
(h0l): h=2n
(h00): h=2n
(0k0): k=2n
(hkl): h+k=2n+1
(hk0): h+k=2n+1
(0kl): k=2n+1
(h0l): h=2n+1
(h00): h=2n+1
(0k0): k=2n+1
PC
(010)
(100)
(011)
(101)
(012)
(102)
(210)
(121)
(210)(013)
(103)
(211)
(122)
(030)
(031)
(212)
Reflection Conditions for Magnetic lattices C and PC
MSERC
The face centred lattice C has ferromagnetics with the general reflection condition is h+k=2n, the same the nuclear one.
The primed face centred lattice PC has antifferromagnetics, i.e. the atom (ion) at (½, ½, 0) is antiparallel arrangement with the one at (0 0 0). The general reflection condition is h+k=2n+1.

## Slide 30
(001)
(110)
(002)
(111)
(112)
(021)
(020)
(003)
(200)
(022)
(201)
(113)
(202)
(220)
C
PC
(010)
(100)
(011)
(101)
(012)
(102)
(210)
(121)
(210)(013)
(103)
(211)
(122)
(030)
(031)
(212)
Mz
My
Example of Reflection Condition of a Canted Magnetic Order
MSERC
The canting face centred lattice C can be divided into two components, along to the c-axis one has ferromagnetics with the general reflection condition of h+k=2n, the same as the nuclear one.
Another component in the b direction has antifferromagnetics (PC), i.e. the atom (or ion) at (½, ½, 0) is antiparallel arrangement with the one at (0 0 0). The general reflection condition is h+k=2n+1.

## Slide 31
(100)
(101)
(110)
(111)
(102)
(112)
(120)
(121)
(103)
(122)
(113)
(130)
(131)
(123)
(010)
(011)
(110)
(111)
(012)
(112)
(013)
(211)
(113)
(030)
(031)
(212)
(001)
(011)
(011)
(111)
(021)
(003)
(103)
(013)
(103)
(211)
(113)
(031)
(023)
Pa
Pb
Pc
(hkl): h=2n+1
(hk0): h=2n+1
(h0l): h=2n+1
(h00): h=2n+1
(hkl): k=2n+1
(hk0): k=2n+1
(0kl): k=2n+1
(0k0): k=2n+1
(hkl): l=2n+1
(0kl): l=2n+1
(h0l): l=2n+1
(00l): l=2n+1
Reflection Conditions for Magnetic Lattices Pa, Pb, and Pc
MSERC

## Slide 32
Integral Reflection Conditions of Centred Magnetic Lattices
MSERC

## Slide 33
Integral reflection conditions of centred magnetic lattices
continues
IC
MSERC

## Slide 34
(x y z)
(Mx My Mz)
(x y z)
(Mx My Mz)
( x y z )
(Mx My Mz)
Moment
Spin
(1) Magnetic moment direction: It is determined by the right-hand rule of spin direction.
(2) Magnetic symmetry operation: Symmetric elements operate on spin units, such as center symmetric operation: A to B.
(3) Perform an inversion operation follows the operating (2), i.e. from B to C, represented by “add a prime on the symmetry element”, such as I’, 2’, 3’, m’, ...
A
B
C
MSERC
Magnetic symmetry elements and corresponding symmetry operations
Reversal
We discus symmetry of magnetics not only the crystallographic elements of symmetry (rotations, reflections and translations) but also the time-inversion element 1’, which causes the reversal of the magnetic moment density vector m.
The operation of time-inversion 1’ (black–white exchange)
Inversion through
the point, 1
_
Inversion through
the point
Then reversal, 1’
_

## Slide 35
If a magnetic element at a symcenter, it magnetic moment will be ZERO.
Used in lattice, screw axis, and glide oparetion
FM
AFM
FM
Inversion and Translation
MSERC
Reversal
AFM
Primed translation t’
Reversal

## Slide 36
A
at axis
A
at axis
Two-fold Axis
MSERC
Primed twofold rotation axis – 2’

## Slide 37
1
2
3
4
1
2
3
4
* If a magnetic moment parallels to a four-fold axis, ferromagnetic is formed through the four-fold axis operation.
* While the moment is perpendicular to the four-fold axis, antiferromagnetic is formed .
* If the moment forms an angle with the four-fold axis, canting magnetic is formed.
* If a magnetic atom is on a four-fold axis and the magnetic moment is perpendicular to the four-fold axis, the moment will be zero.
Four-fold and primed four-fold Axis
MSERC

## Slide 38
1
2
3
4
1
2
3
4
* If a magnetic moment parallels to a 4 axis, ferromagnetic is formed through the 4 axis operation.
* While the moment is perpendicular to the 4 axis, antiferromagnetic is formed .
* If a magnetic atom is on a 4 axis and the magnetic moment is perpen-dicular to the 4 axis, the moment will be zero.
_
_
_
_
4 axis
_
_
Inversion four-fold and primed inversion four-fold axis
MSERC

## Slide 39
*International tables for crystallography, Vol. A, 29 (1992).
MSERC
Zonal and serial magnetic reflection conditions for white and primed magnetic screw axes
=2n+1
=4n+1
=2n+1
=4n+1
=4n+1
=2n+1
=3n+1
=6n+1
=2n+1

## Slide 40
MSERC
Mirror plane and primed mirror plane
Primed mirror plane m’
m

## Slide 41
Glide plane c
a
b
c
1/2c
1/2c
1/2c
MSERC
Mirror Plane + Translation

## Slide 42
MSERC
Zonal and serial magnetic reflection conditions for white glide planes
=2n+1
=2n+1
=2n+1
=2n+1
=2n+1
=2n+1
=2n+1
=2n+1
=2n+1
=2n+1
=4n+1
=2n+1
=2n+1
=4n+1
=4n+1

## Slide 43
MSERC
Zonal and serial magnetic reflection conditions for white glide planes continues
=4n+1
=4n+1
=4n+1
=2n+1
=2n+1
=2n+1
=2n+1
=2n+1
=2n+1
=2n+1

## Slide 44
Pa nma
Pb nma
Pc nma
PA nma
PB nma
PC nma
PI nma
Magnetic space groups under #62: Pnma
* Paramagnetic
*Pnma1’
Pnma
Pn’m’a
Pnm’a’
Pn’ma’
Pn’m’a’
Pn’ma
Pnm’a
Pnma’
Magnetic space group
M-space group

## Slide 45
Summary
Magnetic neutron diffraction contains all the magnetic structure information, including ordered magnetic moment and the symmetry of magnetic structure, etc.
Magnetic cell is highly correlated to the nuclear unit cell (VM =nVN, n=1, 2, 3, 4...).
The symmetry of magnetic structure is developed based on the symmetry of crystal structure .
By using the magnetic neutron diffraction intensity data, one will be able to get the ordered magnetic moment magnitude, direction, and arrangement in a magnetic unit cell.
Magnetic neutron diffraction is independent of crystal diffraction and can therefore be refined as an independent phase.

## Slide 46
Thank you FOR YOUR ATTENTION!
As experimental equipment, theoretical understanding, and computation tools/software have improved and developed, it has become possible to modeling and refining magnetic structure from neutron powder diffraction, despite a limited number of magnetic diffraction peak and/or weaker peak intensity.

## Slide 47
In the dipolar approximation:
International Tables of Crystallography, Volume C,
ed. by AJC Wilson, Kluwer Ac. Pub., 1998, p. 513
Magnetic form factor

## Slide 48
Fhkl = |∑ bj exp(2p i (hx + ky + lz)) |2 e-2W
Nuclear fit only
Magnetic diffraction intensities
A plot of neutron diffraction intensity pattern fitted with nuclear structure model only (red line). The differences, shown at the lower part of the plot, are the magnetic diffraction intensities (blue line) .
Magnetic: Fhkl = |∑ qj fMj exp(2p i (hx + ky + lz))|2 e-2W
2
Nuclear and Magnetic Neutron Diffraction
M-diffraction
2
Magnetic form factor is a function of (sinq )/l.

## Slide 49
Diamagnetic c < 0
Electrons paired to form bonds;
Weak magnetic induction;
Small negative susceptibility;
Cause small orbital changes;
The material is driven away
by external magnetic forces.
Paramagnetic c > 0
The element has unpaired electrons;
Moment orientation disorder;
The magnetic order can be induced when a external magnetic field applied;
Magnetization is linearly
proportional to the external field.
Schematic diagram
Spin disorder: Paramagnets & Diamagnets
If integral magnetic moment is identically equal to zero ( ≡ 0) at every point, the substance is a disordered magnetic. There are two types of such magnetics: paramagnets and diamagnets.
MFM

## Slide 50
Antiferromagnetic
Adjacent moment are antiparallel
相邻自旋反平行
The net magnetic moment under a zero field is zero
零场下净磁矩为零
A small influence by an external magnetic field applyed
外加磁场影响小
Néel (order) temperature TN
相变温度TN， Néel温度
Schematic diagram
Spin order: Antiferromagnet
  The magnetization of an antiferro-magnetic (AFM) order temperature TN drops down.
When integral magnetic moment is equal to zero at every point, such a substance is called antiferromagnetic. The integration is performed over the magnetic elementary cell, which may differ from the crystallographic one.
MFM

## Slide 51
FM
T (K)
TC
PM
A magnetization curve for a ferro-magnetic order shows hysteresis.
Spin order: Ferromagnets (& Ferrimagnets)
Ferro- and ferrimagnetic
The moment are parallel
自旋平行排列
Spontaneous magnetization
自发磁化
The external magnetic field has great influence
外加磁场影响大
Hysteresis under applied temperature, magnetic, and pressure field
温度和磁滞后现象
Curie (ordering) temperature TC
相变温度TC， Curie温度
The integral magnetic moment is not zero over the primitive cell, such a substance is called ferromagnetic. The ferromagnetic possesses only one kind of magnetic ion or atom. All their magnetic moments are aligned parallel to each other in the same direction. The ferromagnets are divided into two groups: one-sublattice ferromagnets and multisublattice ferro- and ferrimagnets.
ferromagnetic
ferrimagnetic
MFM

## Slide 52
Magnetization may be changed by changing chemical composition and temperature, and applying external magnetic field or pressure, etc. Therefor, to understand the magnetic structure is necessary for understanding the relationship between magnetic structure and property. The neutron diffraction can help us to
Different kinds of Magnetization Curve
MFM

## Slide 53
+ e
0 e
+e
Neutron, A Subatomic Particle
Introduction
Neutron
one “up” quark (charge +2/3e)
two “down” quarks
(charge −2/3 e)
All matters are composed of tiny particles call atom. Every atom is made up of three types of smaller subatomic particles, electron, neutron, and proton. Proton and neutron make up nucleus, surrounded by electrons.
The proton carries two “up” quarks and one “down” quark, while the neutron carries one “up” quark and two ‘down” quarks. The “up” quark have +2/3 e, and the “down quark has -1/3 e. So that the proton carries +e, and the neutron is a neutral particle.
Proton
two “up” quarks (charge +4/3 e)
one “down” quark (charge -1/3 e)
+e
0e
+2/3e
+2/3e
+2/3e
-1/3e
-1/3e
-1/3e

## Slide 54
Theorized | Ernest Rutherford (1920)
Discovered | James Chadwick (1932)
Mass | 1.67492749804(95)×10−27 kg, 939.56542052(54) MeV/c2, 1.00866491588(49) Da
Mean lifetime | 879.4(6) s (free)
Electric charge | 0 e (−2±8)×10−22 e (experimental limits)
Electric dipole moment | < 2.9×10−26 e⋅cm (experimental upper limit)
Electric polarizability | 1.16(15)×10−3 fm3
Magnetic moment | −1.04187563(25)×10−3 , −1.91304273(45)
Magnetic polarizability | 3.7(20)×10−4 fm3
Spin | 1/2
Wavevector | Magnitude 2p / l
Wavelength | h/mv
Energy (E) | (1/2)mv2=h2/2ml2
mB
mN
Intrinsic Properties of Neutron, Wave-particle Duality
中子的本征性质， 波粒二象性
Introduction
The most mass of an atom comes from proton and neutron. The mass of a neutron （1.67492749804(95)×10−27 kg）is slightly greater than a proton.
Neutrons accompany protons in nucleus. When neutrons leave nucleus become free, the average lifetime of a free neutron is about 14.66 minutes.
Although neutron is a neutral particle, it carries zero electric charge. The magnetic moment of neutron is not zero.
It has spin ½ with moment of -0.001042 mB.
This is an indication of its quark substructure and internal charge distribution.
Energy E= ½ mv2=h2/2ml2, that is the lower v the lower E or the shorter l the higher E.
Neutrons move in a wave mode; the wavelength l=h/mv, i.e. the higher v the shorter l.
The magnitude of wavevector (2p / l) is a function of wavelength.
Neutrons possess wave-particle duality.

## Slide 55
为什么用中子？中子有揭示了其他探针无法获得的特性的能力。它可以像波一样衍 射或反射，或者像粒子在运动过程中与物质碰撞时获得或失去能量。
波长 从0.1A到100A不等，允许它们测量从像原子一样小到蛋白质一样大的结构。
能量 在毫电子伏特量级，与固体或液体中原子运动，磁性材料中的波或分子振动 的能量相同。可以检测的小的纳米电子伏特和十分之一电子伏特的中子与物质 之间的能量交换。
散射本领 几乎随机地因原子核而异。有利于对探测轻的原子，同位分离等。
磁性 使得中子对原子中的电子自旋和电子的轨道自旋的有序度都很敏感。
穿透能力强 中性的中子使得其能够深入样品，更容易穿过极端条件环境设备壁达 到样品，如测量桥梁中的应力应变。
中子的优势特点
Introduction

## Slide 56
Elastic and Inelastic Scattering
When atoms in a solid are of finite mass and they do or don’t gain or loss energy when neutrons, or any kind of radiation, collide with them.
Neutrons scattering from a sample have the same energy as the incident neutrons.
The neutrons gain or lose some energy as scattering from a sample.
Wave
Particle
Introduction

## Slide 57
*International tables for crystallography, Vol. A, 15 (1992).
M-space group
Lattice symmetry directions for three dimensions

## Slide 58
Magnetic intensities
Magnetic intensities
transition metal
rear-earth element
有序磁结构的中子衍射
(1)The magnetic form factor makes the magnetic diffraction peaks appear at a lower angle region.
(2)The magnetic phase can be treated as an independent phase duing refinement.
Mn3+ form factor
Er3+ form factor
LaMnO3
Magnetic diffraction and form factor for transition metal and rear-earth elements
(a)
(a’)
(b)
(b’)
Introduction

## Slide 59
P
W&B Magnetic Lattice
磁结构点阵, 磁单胞

## Slide 60
A
C
I
F
磁结构点阵, 磁单胞
W&B Magnetic Lattice

## Slide 61
Peaks Position: 2dhkl sinqhkl = nl
where l is the incident beam wavelength, d and q are the distance between successive hkl planes and Bragg angles of reflections, respectively.
Diffraction Intensity: Ihkl = CFhkl
where Fhkl is the hkl reflection amplitude of the diffracted X-ray, or neutron, or magnetic, and C is all others.
X-ray: Fhkl = |∑ fj exp(2p i (hx + ky + lz))|2 e-2W
where fj is the atomic scattering factor of atom j for X-ray.
Neutron: Fhkl = |∑ bj exp(2p i (hx + ky + lz))|2 e-2W
where bj is the neutron scattering length for atom j.
Magnetic: Fhkl = |∑ qj fMj exp(2p i (hx + ky + lz))|2 e-2W
where qj and fMj are the magnetic interaction vector and the
magnetic form factor for atom j, respectively.
NPD
In polycrystalline diffraction, the positions of diffraction peaks for both nuclear and magnetic obey the Bragg equation, and the expression of structure factors are similar.
2
2
2
2
1. Peak position: d =l/ 2sinq
2. Peak intensity: Ihkl=C|Fhkl|2
3. Structure factor: Fhkl
Position, Intensity, and Structure Factor for XRPD & NPD Powder Diffraction

## Slide 62
c is the magnetic susceptibility, for paramagnets it follows the Curi-Weiss law in low magnetic field (mBB<<KBT):
FM
T (K)
TC
PM
0
q
q  0: FM
q  0: AFM
Introduction
Magnetization
A
B
C
A: A magnetization curve for a ferromagnetic (FM) ordering. It shows hysteresis;
B: A magnetization curve for an antiferromagnetic (AFM) ordering. It shows at the order temperature TN where the magnetization drops down;
C: The temperature dependence of the inverse magnetic susceptibility 1/c for different types of magnetic ordering. When q > 0: FM
q < 0: AFM

## Slide 63
|FM |2 = |å m f exp(2pi(hx + ky + lz))|2 e-W
If h = k = l = 0 , exp(2pi(hx + ky + lz)) =1, and f =1, then FM (000) = å m
S-order intensities
0
0
2q
中子粉末衍射研究结构和性能关系
Using SANS to find Short-range FM I(000) peak
100 nm (100%)
100 nm (50%)+11 nm (50%)
100 nm (80%)+11 nm (20%)
|FM|2
M-diffraction

## Slide 64
Plot of the SANS integrated intensity (between Q range between 0.04 and 0.2) vs temperature appears a peak at the position near the Tcant of ~200 K, confirming the present of the SFM above ~200 K.
The SFM order confirmed by measuring
the (000)FM diffraction
SANS data at low Q for La(Fe11.5Al1.5)
SANS integrated intensity
M-T
Cell
parameter
M-diffraction

## Slide 65
Reflection condition Symmetry element
I (0k0) =0 2 (//b-axis & M)
0k0: k =2n+1 21 (//b-axis & M)
0k0: k =2n 21’ (//b-axis & M)
I(00l) =0 3, , 3’,4, , 4’, ’, 42, 2’,
6, 62, 63, 64 (//c-axis & M)
00l: l =2n+1 41, 41’, 43, 43’ (// c-axis &M)
00l: l =3n 31, 32 (//c-axis & M)
00l: l =3n 61, 65 (//c-axis & M)
In addition to systematic absences, can also be observed when the condition Fhkl = 0 occurs because the magnetic spin K is parallel to the scattering vector e for a class of reflections hkl. In this case the angle a between the scattering and the magnetization vectors is zero, and, consequently, |q|=sina=0.
磁结构衍射条件和消光规律
?
The reflection condition of rotation axes
when magnetization vector K is parallel the scattering vector
MSERC

## Slide 66
Two-Fold Axis
Mirror Plane
MSERC

## Slide 67
M-super-cell
N-cell
a
c
1. One has to set the magnetic phase to be a new phase due to the enlarged magnetic unit cell is defferent to the nuclear one;
2. Only the magnetic atoms are included in the magnetic phase and only the magnetic diffractions are included in the calculation;
3. The magnetic structure becomes orthorhombic system.
AFM: M-cell has an Enlarged cell
M-cell

## Slide 68
*
* Triclinic & Cc
in Hexagonal
# Monoclinic
#
Types of magnetic lattice
a
b
c
The first low in Fig. b (White) shows the lattice types that appear in the nuclear structure, and in magnetite structure as well. The lattice points in each lattice are equivalence, they can be used to describe a ferromagnetic structure. The rest lattices in Fig. b are used to described the anti-ferromagnetic ordering structure (White & Black) , due to the anti spin is introduced.
图中左侧第一列所示的是在晶体结构中常见简单的和有心的点阵类型。因为在这类晶胞中所有的阵点都是等效的，所以可以用在描述具有铁磁排列的磁结构单胞（white）。然而，在引入反铁磁排列后，就衍生出多种新的磁晶胞类型（white & black）。
磁结构点阵, 磁单胞
The 14 crystal Bravais lattices
In 14 Bravais nuclear lattices（Fig. a) there are three centred-lattices: C/B/A-face-centred (C), body centred (I), and all-face centred (F). 在14个Bravais 点阵中只有3种有心类型：底心，体心和面心。
White & Black
White Ps Pa Pb Pc
P
PI PA PC
C Ca Cc CA
A Aa
F Fs
I IC
R RI
a
b

## Slide 69
International Table for crystallography (2006), Vol. D, Chapter 1.5, P112
List of the magnetic classes in which ferromagnetism is admitted
M-space group

## Slide 70
1651 magnetic (Shubnikov) space groups
Generated by combining the 36 magnetic lattices and magnetic symmetry
M-space group
N.V.Belov, N.N.Neronora and T.S.Smirnova, Soviet Physics, Crystallography, Vol. 2, #3, 311-322(1957)

## Slide 71
1651 magnetic space groups continue
M-space group

## Slide 72
1651 magnetic space groups continue
M-space group

## Slide 73
1651 magnetic space groups continue
M-space group

## Slide 74
1651 magnetic space groups continue
M-space group

## Slide 75
For each Wyckoff position the triplets h, k, l are divided into two sets:
(1) triplets for which the structure factors are systematically zero (extinctions);
(2) triplets for which the structure factors are not systematically zero (reflections).
Conditions that define triplets of the second set are called reflection conditions.

## Slide 76
<1-(t · M)2>:orientation factor
When a increases from 0 to 90 degree, the (|q|=sina) increases from 0 to 1.
f : magnetic form factor
Magnetic form factor is a function of (sinq)/l.
1.0
0.2
0.4
0.6
0
0.8
1.0
0.4
0.6
0
0.2
0.8
Moment (mB)
mB
2
m : magnetic moment
Fhkl = |å m f exp[2p i (hx + ky + lz)]|2e-W
2
Introduction

## Slide 77
1651 Magnetic Space Groups
M-space group
1651 magnetic space groups divide into three types
Type I: 230 trivial magnetic space groups that describe diamagnetic and paramagnets. Which consists of the 230 crystallographic space groups to which 1’ is added. Crystals show no magnetic order.
Type II consists of the same 230 crystallographic groups which do not include 1’ in any form. The magnetic unit cell coincides with the classical one. 44 groups describe different ferromagnetic crystals and 186 are antiferromagnets.
Type III: There are 1191 nontrivial magnetic space groups, in which 1’ enters only in combination with rotations, reflections or translations. There are 674 magnetic space groups of subtype that the 1’ is not combined with translations, and 231 of them admit ferromagnets and the 443 describe antiferromagnets.

## Slide 78
*A. S. Borovik-Romanov† and H. Grimmer. Magnetic properties. International Tables for Crystallography (2006). Vol. D, Chapter 1.5, pp. 105–149. *Daniel B. Litvin. Magnetic Space Group Types. (2010) & Points Group Symmetries (2001)
Symbols of crystal families | Crystal system | Conditions imposed on cell geometry
 | Triclinic | None
m | Monoclinic | a = g = 90° (b unique); a =b =90° (c unique)
o | Orthorhombic | a = b = g = 90°
t | Tetragonal | a=b; a = b= g = 90°
h | Trigonal | a=b; a = b = 90° ; g = 120° (hexagonal setting) a=b=c; a = b = g (rhombohedral setting)
h | Hexagonal | a=b; a = b = 90°; g = 120°
c | Cubic | a=b=c; a = b = g = 90°
Symbols of crystal families | Crystal system | Conditions imposed on cell geometry
 | Triclinic | None
m | Monoclinic | a = g = 90° (b unique); a =b =90° (c unique)
o | Orthorhombic | a = b = g = 90°
t | Tetragonal | a=b; a = b= g = 90°
h | Trigonal | a=b; a = b = 90° ; g = 120° (hexagonal setting) a=b=c; a = b = g (rhombohedral setting)
h | Hexagonal | a=b; a = b = 90°; g = 120°
c | Cubic | a=b=c; a = b = g = 90°
Unit Cell Notation
The unit cell is the smallest repeating unit in a crystal structure.
MSERC
Notations of Nuclear & Magnetic Crystal Families and Cells
The crystal families are symbolized by the lower-case letters a, m, o, t, h, and c.
All ‘hexagonal’, ‘trigonal’ and ‘rhombohedral’ space groups are contained in one family, the hexagonal crystal family.

## Slide 79
S. F. Jin, Q. Huang, Z. P. Lin, Z. L. Li, X. Z. Wu, T. P. Ying, G. Wang, and X. L. Chen. PHYSICAL REVIEW B 91, 094420 (2015)
有序磁结构的中子衍射
AFM with
propagation
vector (u v w):
(½, ½, 0)
M-cell:
2a x 2b x c
Short-range, 2-dimension, and long-range magnetic order
M-diffraction

## Slide 80
KxFe2-ySe2 superconductor
Structure at high-T: I4/mmm, a=b, c
Sup-structure at low-T: I4/m, aS=bS=5×a; cS=c
Magnetic space group: I4/m’, aM=bM=5×a, cM=c AFM with Fe moment along the c-axes.
I4/mmm
Nuclear: I4/m
Magnetic: I4/m’
1. Magnetic peaks can be indexed using nuclear unit cell;
2. All magnetic peaks have h+k+l=2n, indicating that M-cell has body center.
有序磁结构的中子衍射
h+k+l=2n
AFM: M-cell has the same as the N-cell
M-cell

## Slide 81
Tamperature dependent of magnetic diffraction
GeCo2O4
at 8 K
Nulear fit only
Counts
The peak intensity decreases with the increase of temperature，and the peak disappears above the magnetic order temparature ~20 K.
Fitted with fixed Background
M-diffraction

## Slide 82
Magnetic peaks can be indexed by nulear unit cell constants
Subtraction
AFM: M-cell is the same as the N-cell
a
b
c
d
a & b: Material is paramegnetic at 300 K and 150 K, respectively.
c: Some new peaks are observed at 50 K, and all new peaks can be indexed using the nulear unit cell dimension.
d: A plot of difference by subtracting data at 150 K from the data at 50 K shows the orderded magnetic intensies.
AFM
aM = aN
bM = bN
cM = cN
M-diffraction

## Slide 83
The unit cell is the smallest repeating unit in the crystal structure. The magnetic unit cell may be or may not be consistent with the nuclear unit cell.
The magnetic unit cell of ferromagnetism is the same as that of crystal;
(2) The unit cell volume for antiferromagnetic would be VM=nVN, n=1, 2, 3, 4..., where VM and VN is the magnetic cell and crystal cell, respectively.
(3) For incommensurate magnetic, its cell volume VM>VN, i.e. there is no integer multiple relationship between the two.
Cell
notation
Nuclear & Magnetic Unit Cell
MSERC

## Slide 84
3d series
Transition metal
4f series
Rear-earth
4d
5d
5f
Periodic Table
MFM
In principle, all elements are magnets, but only elements those having unpaired electrons may appear macroscopic magnets when the spin and orbital of unpaired electrons are in some way ordered, such as elements having 3d, 4d,5d 4f, and 5f unpaired electrons. The 3d trasition metal and 4f rear-earth elements, alloys, and compounds have been investigated the most.

## Slide 85
Transition metals: 3d, 4d, series, Rare earth: 4f series ; Radioactive rare earth: 5f series
Ferromagnetic, Ferrimagnetic, Antiferromagnetic,
Elements
Type of magnetism
Inorganic and Organic compounds, Metals, and Alloys, etc.
Discipline
Physical property
Magnetostatic
Permanent magnetic; Soft magnetic;
Rectangular magnetic;
Magnetic record; etc.
Magnetic-propertiy Coupling
Magneto-optical; Magnetoelestic; Magnetocaloric; Magnetoresistant; Magnetostriction; Gyromagnetic；
Anomalous Hall Effect; Spintronic; etc.
Amorphous
Nano-crystal
Micro-site crystal
Crystalline type
Bulk, Film, Single crystal
Application
Introduction
Widely used in: Communication, Transportation, Information storage, Medical devices, Scientific equipment, and Military science, etc.
Magnetism in Material Science
MFM
The most common forms of magnetic order are FM and AFM, along with various properties that people care about and to kwon the relationship between magnetism and properties, it is necessary to understand the ordered magnetic structure.
(1)